**TECHNICAL DATA SHEET**

ENG-AU-BLA-180CB

**SIGNATURE AUSTRALIAN RANGE: BLACKBUTT CHARACTER SATIN**

**PRODUCT SPECIFICATIONS**

|  |  |  |
| --- | --- | --- |
| PRODUCT RANGE | SIGNATURE AUSTALIAN RANGE | The photograph used in this sheet is intended as an illustration. It does not provide any indication of grading. Colours will vary between batches in stock. |
| COLOUR | BLACKBUTT |
| PRODUCT CODE | ENG-AU-BLA-180CB |
| CONSTRUCTION | MULTI-LAYERED ENGINEERED |
| BACKING | EUCALYPTUS PLYWOOD |
| GRADE | CHARACTER |
| PATTERN | 1 STRIP |
| BOX SIZE | VARIES WITH BATCH |
| EDGE | BEVEL |
| PROFILE | TONGUE AND GROOVE |
| FINISH | LACQUER |
| TOP LAYER | 3mm BLACKBUTT LAMELLA |
| THICKNESS | 14mm |
| WIDTH (mm) | 180 |
| LENGTH | 1900mm (Product contains split lengths, with up to 25% shorter boards. These may be half or 1/3 lengths) |

**INSTALLATION METHODS**

|  |  |
| --- | --- |
| DIRECT STICK | YES |
| FLOATING ON UNDERLAY | YES |
| OVER UNDERFLOOR HEATING | YES WITH LIMITATIONS |

**AUSTRALIAN STANDARDS**

|  |  |
| --- | --- |
| ACOUSTIC RATING | DEPENDENT ON UNDERLAY |
| SLIP RATING  AS 4586-2013 | P2 |
| FORMELDELHYDE RATING | E1 |
| CRITICAL HEAT FLUX (CHF) MEAN  AS/ISO 9239.1-2003 | 3.2 kW/m2 |
| JANKA HARDNESS RATING | 9.1kN |

**WARRANTY**

|  |  |
| --- | --- |
| RESIDENTIAL | LIFETIME STRUCTURAL |
| COMMERCIAL | 10 YEARS STRUCTURAL |

****